



**01793 511000**

Mon-Thurs 9:00 - 17:00

Fri 9:00 - 14:00

**sales@bondline.co.uk**

www.bondline.co.uk

**PLASTIC PACKAGING TAX 1st APRIL 2022**

**MOISTURE BARRIER BAGS CONSTRUCTION (MOI)**



|  |  |
| --- | --- |
| Construction | Values |
| Structure | PET/AL/PE (0.1mm, 123gsm) |
| PET | 0.012mm, 17gsm (13.82%), 100% Reusable |
| AL | 0.007mm, 19gsm (15.45%), 100% Reusable |
| PE | 0.08mm, 74gsm (60.17%), 100% Reusable, (39gsm Recycled, 52.71%) |
| Glue + Antistatic Coating | 0.003mm, 2gsm, 1.63% |
| Proportion of the recycled material | 39/123= 31.71% |

Victoria Blizzard

Director

01.03.2022

**A picture containing surface chart

Description automatically generated**

**© Copyright** Bondline Electronics Limited. **Registered Company Number:** 02933918.

**Registered Company Address:** Bondline Electronics Limited, Unit 4 Rivermead Dr, Swindon, Wiltshire, SN5 7EX.

**Telephone:** 01793 511000 **Website:** www.bondline.co.uk **Email:** sales@bondline.co.uk