Specification of Precision Tweezers

General

Made of Stainless steel

(Low carbon austenitic steel material number 1.4404 DIN X2CrNiMo 17-12-2 AISI number 316L Thyssen steel)

Contains from 16.5 to 18.5 wt% chromium and has important quantities of nickel and molybdenum as additional alloying elements.

Non-magnetisable.

Good corrosion resistance and toughness are primary requirements.

Typical applications include tools and equipment for laboratory and medical applications in mild aggressive chemical environments.

Composition:

| Component C P Mo | Wt % <0.03 <0.045 2.0-2.5 | Component Si S Ni | Wt% <1.0 <0.03 10.0 – 13.00 | Component Mn Cr | Wt% <2.0 16.5 – 18.5 |
| --- | --- | --- | --- | --- | --- |

Mechanical Properties:

State			Annealed

Density			8.0 g/cm3

Hardness HB30		<215

Hardness Rockwell B	79

Tensile strength ultimate	500-700 MPa

Tensile strength yield	290

0.2% Yield stress		>200 MPa

Elongation, break		40%

Modulus of elasticity	200 GPa

Thermal Properties:

Coef of lin therm expansion 	16.0 E-6/degrees C	20-100 degrees C

Coef of lint herm expansion 	17.0 E-6/ degrees C	20-300 degrees C

Specific heat capacity:		0.50J (g.K)

Thermal conductivity:		15W/m.K)

Continuous use temperature:	300 degrees C

Max service temperature, air	825 degrees C

Electrical Properties

Resistivity: 			0.75 E-4 ohm.cm

The information contained within this spec sheet is for guidance only. We make no warranties expressed or implied and assume no liability regarding any use of this information.(Re-view July 15)